## Slide 1: VLSI Technology To Manufacture High Density Thermoelectric Cooling Devices
by
S.Raghavendra
Roll no:19

## Slide 2: Abstract:-
This presentation describes a novel integrated circuit technology to manufacture high-density thermoelectric devices on a semiconductor wafer.
With no moving parts, a thermoelectric cooler operates quietly, allows cooling below ambient temperature.
This may be used for temperature control or heating if the direction of current flow is reversed.
The solid state technology can be combined with traditional air cooling, liquid cooling and phase-change cooling to yield greater heat flux and provide better cooling capability.

## Slide 3: Traditional thermal technology:
The International Technology Roadmap for Semiconductors predicts that power dissipation and thermal problems are major design challenges to continued scaling.
To meet the power demand of each application, today’s prevailing cooling technologies can be divided into 4 categories:
1.Natural air convection,
2.Forced air convection,
3.Fluid phase change
4.Liquid cooling.

## Slide 4: Principle of thermoelectric cooling:-

## Slide 5
The principle of heat transfer in a thermoelectric module can be explained by the Peltier Effect.
As a result of seeback effect, the thermoelectric module can be used for power generation, where a current is generated due to the temperature differences across the thermoelectric module.

## Slide 6: Characteristics of thermoelectric cooling devices:-
The characteristics of the thermoelectric cooling module are light-weight, maintenance-free, and environmentally friendly.
With no moving parts, it is also acoustically silent and electrically quiet.
A thermoelectric module can provide active heating and cooling in the same device with precise temperature control (within 0.1 °C).
It can also operate in a wide range of temperatures, from sub-ambient cooling to low temperature (-80 °C) cooling.

## Slide 7: Thermoelectric material:-
The ideal Peltier cooling rate of a thermoelectric module is equal to Qp = π. I= α.Tc. I ,
The heat will also be conducted from the hot plate back to the cold plate. The Fourier heat conduction rate is equal to Q c =κ ⋅ Δ T,
In addition, there will be Joule heating, which equals ½ ⋅ I ⋅ R2
The net cooling rate of a thermoelectric module can be calculated from the following formula
Notes: <number>

## Slide 8
In order to increase the Peltier cooling rate and reduce the back flow of Fourier heat conduction from hot plate to cold plate, thermoelectric material must exhibit a high Seebeck coefficient, low thermal conductivity and low electrical resistance.
For example, metal alloys are known to have high thermal and electrical conductivities, but since their Seebeck coefficients are inherently low, metals are not suitable fort hermoelectric cooling.
On the other hand, extrinsic alloysemiconductors are known to offer reasonable electric conductivity while maintaining low thermal conductivity. They also exhibit relatively large Seebeck coefficients and narrow band gap.
These semiconductor alloys include zinc antimonite, indium antimonite, lead telluride, bismuth telluride, silicon germanium (SiGe), and Li-Ni-O compounds.

## Slide 9: Processing Steps to Form Thermoelectric Array:-
The heat pumping capacity of a thermoelectric cooling module can be improved by increasing the number of thermoelectric couple elements and arrays.
Therefore, the reduction of the feature sizes of thermoelectric couple elements using advanced thin-film material and technologies will lead to significant improvement in the heat pumping capacity of the thermoelectric cooling module.
In this section, we propose a new technology to form thermoelectric (TE) couple elements on a bulk silicon or SOI substrate.

## Slide 10
First, a layer of dielectric material (SiO2) is deposited on the surface of an SOI wafer by using a plasma-enhanced tetraethyl-ortho-silicate (TEOS) deposition process. The thickness of the TEOS oxide layer will determine the height of the thermoelectric cooling couple elements.
Notes: <number>
First, a layer of dielectric material (SiO2) is deposited on
the surface of an SOI wafer by using a plasma-enhanced tetraethyl-
ortho-silicate (TEOS) deposition process (Fig. 2a). The
thickness of the TEOS oxide layer will determine the height
of the thermoelectric cooling couple elements.

## Slide 11
A photolithography process is then used to define the array
patterns of thermoelectric couple elements (Fig.b), followed
by an Etching process to create the structural voids needed in
the dielectric and the silicon layers to form arrays of
thermoelectric couple elements (Fig.c).

## Slide 12
A chemical vapor deposition (CVD) process is used to deposit a second dielectric material such as nitride to fill the voids (Fig. a).
The top surface of the CVD nitride is planarized and flushed with the top surface of the first dielectric material (TEOS oxide). The first dielectric material (TEOS oxide) is then selectively removed by using reactive ion etching (RIE) technique to create a three-dimensional structure where the thermoelectric cooling material can be deposited (Fig. b).
The sidewalls of the second dielectric material (CVD nitride) can be tapered with a desired angle (between 75° and 90°), using controlled wet etching to facilitate the ensuing angle implantation (Fig. c).

## Slide 13
* Angle implantation has the advantage of not requiring any photo mask, the thermoelectric materials along the sidewalls are properly annealed to form the n-type and p-type thermoelectric couple elements.
* The newly formed n-type and p-type thermoelectric elements on the sidewalls of CVD nitride are insulated and covered with nitride spacers (Fig. 4b).
* The exposed top and bottom parts of the SiGe epitaxial layer are converted into metal silicides by a self-aligned silicidation process. The top and bottom metal silicides are used as low-resistance contacts to electrically connect the adjacent p-type and n-type thermoelectric couple elements.

## Slide 14
* A thick layer of insulating material can
be deposited on the top of the structure by using TEOS-based SiO2 to cap and protect the thermoelectric device (Fig. 5a).
* Array structures of the thermoelectric cooling couple elements can now be formed by a photolithographic patterning process, followed by an etching process to remove the metal silicides, SiGe thin films, and the sidewall spacers between adjacent rows of thermoelectric couple elements (Fig. 5b). As the etching stops at the buried oxide layer, arrays of high-density thermoelectric cooling elements are formed.

## Slide 15: Integration of Thermoelectric Cooling Module:-
The use of a high-density thermoelectric module allows cooling to take place inside the chip. The integration of thermoelectric cooling devices on a chip requires an effective means such as air cooling by heat sink or liquid cooling through micro-channels to remove the heat from thermoelectric couple elements.
To facilitate various heat removal requirements, one method to integrate thin-film thermoelectric cooling elements on the chip.

## Slide 16
where an integrated thermoelectric cooling module is bonded to a chip. The integrated thermoelectric cooling module consists of arrays of thermoelectric couple elements fabricated separately on the front side of an SOI wafer, while the heat sink or micro-channel devices can be attached to the backside of the substrate. After planarization and the removal of the original silicon substrate, the completely integrated thermoelectric cooling module can be glued to the backside of a semiconductor chip using thermal paste

## Slide 17: Thermal simulation:-
The main components of the thermal resistance network include the bulk silicon resistance θsi, the thermal interface resistance θTIM1 between the chip and the TE cooler, the thermal interface resistance θTIM2 between the TE cooler and the external heat sink, and the resistance of the external heat sink θext (Fig. 7). The thermoelectric cooler is characterized by its cold-side heat flow Qc , hot-side heat flow Qh , the cold-side temperature Tc ,and hot-side temperature Th. In addition, the input electrical power needed to provide thermoelectric cooling is represented by Qe.

## Slide 18
the cooling capacity of the TE cooler is
The required input electrical power is
To balance the energy from (1) and (2), the heat rejection on the hot side of the TEC can be derived as
Assuming one-dimensional heat transfer, the hot-plate temperature is

## Slide 19
and the cold-plate temperature is
The parallel thermal conductance of the n-type and p-type TE elements is

## Slide 20
Fig. 9 shows that for a given power density (50 W/cm2), an optimum current can be applied to maximize the benefit of the thermoelectric cooling.
In addition, Fig. 9 shows that as the input current increases, the coefficient of performance (COP) decreases. Therefore, although there are two current values that might deliver the same cooling effect, the lower current will always provide a better COP.

## Slide 21
Fig. 10 shows the TEC cooling effects for different power densities at their respective optimum current conditions. Since the efficiency of Peltier cooling is limited by the Fourier heat conduction and Joule heating, the benefit of using a TEC diminishes when the power density exceeds 120 W/cm2.

## Slide 22: Conclusion:-
A new VLSI integration technology is proposed to achieve greater thermal efficiency with a high-density thin-film thermoelectric cooling module, where millions of thermoelectric couple elements are built on a semiconductor wafer.
By using a mask-less doping technique, n-type elements are formed with a first angle implant using n-type dopants, and p-type elements are formed with a second angle implant using p-type dopants.
The high-density thermoelectric arrays can be implemented directly on the backside of a semiconductor chip, embedded near the hot spots, or fabricated separately on a module.
Combined with traditional heat sinks, micro channels, and heat pipes, the thermoelectric micro-coolers could significantly increase cooling capacity and provide a promising solution to the increasing power demand and thermal design challenges.

## Slide 23
QUIRES…?

## Slide 24
THANK YOU